Literature for Journal Article

Allahverdi et al. 2015:

This article discusses a temperature-age model for prediction of compressive strength for a strange type of concrete: Activated High Phosphorous Slag Cement (PHS).

They use linear regression to fit a logarithmic curve to the strength data collected on PHS that is cured in lime-water bath at 25, 45, 65, 85, and 100 °C.

One of the only papers that doesn’t use degree of hydration.

Alsalman et al. 2017:

USACE 1994:

A finite element analysis was used to account for complex geometry, loading, thermal stresses, nonlinear material behavior, and sequential construction. SEQUENTIAL

Feasibility of a project can be evaluated as well as cracking potential.

Azhena et al. 2009:

Ballim 2004:

Bentz et al. 1998:

Bombich et al. 1991:

The model simulates placement of incremental stages of concrete in a structure and provides other user-defined subroutines to model heat evolution of cement in the concrete mixture.

A user-defined aging creep material model, UMAT, is included to account for change in concrete material strength, modulus of elasticity, creep, shrinkage, etc. and contains a cracking model to evolve the onset and effects of cracking.

Carino 1984:

Cervera et al. 1999:

They provide a decent description in the introduction of how durability and functionality of a concrete structure can be controlled and monitored using a thermo-chemo-mechanical model.

The maximum hydration rate corresponds to the inflection point on the temperature rise curve.

“There is experimental evidence that the evolution of the concrete strength depends not only on the degree of hydration, but also on the kinetics of the hydration reaction.”

“This effect of the curing temperature cannot be reproduced by aging models based exclusively on the hydration degree, or, alternatively, on the concept of maturity or equivalent age.”  supports our model!

Cervera et al. 1999 (2):

A continuation of the previous article applied to damage and creep evolution.

Uses “micro-prestress solidification” to represent long-term mechanical behavior (creep) and a continuum damage model for short-term mechanical behavior.

Might not be needed for this journal article.

Cervera et al. 2002:

Just pretty much put them in group quotes for modeling temperature evolution and chemical affinity.

This paper expands on the Cervera et al. 1999 articles and applies the mathematical formulation to an FEA.

“However, as demonstrated … much experimental observation puts into evidence that concrete strength is affected not only by the accumulative temperature history but also by the history itself.”  Supports our model that doesn’t use maturity!

Gives good explanation of cross-over behavior in section 3.

Continues the discussion started in Kim et al. 1998!!! They compare their model predictions to experimental data for the Kim temperature steps.

D’Aloia et al. 2002:

Di Luzio and Cusatis, 2009:

This study models cement hydration using a complex formulation of time dependent quantities and concentration of important chemical parameters affecting the temperature strength of concrete.

This study focuses on the constituents of High Strength Concrete and the inclusion of the pozzolanic reaction of silica fume.

The hydration reaction is modeled using asymptotic hydration degree based on a mass balance of moisture. Hydration degree is developed for both cement and silica fume.

“As a consequence of the aforementioned volume changes, uniform and/or non-uniform stress states develop in concrete even in the absence of external loads.”  TAKE THAT COUSSY HYPOTHESIS #4

Silica fume promotes strength development through pozzolanic reaction as well as accelerating silicate polymerization.

Great description of moisture transport, heat generation by cement and silica fume, cement hydration, silica fume reaction, and silicate polymerization!

“Ideal hygrometric conditions are never met.” In other words, full hydration of cement can never be achieved because of physical limitations of the moisture transport in a concrete system.

Rate of hydration degree modified for humidity by introducing a factor into dαc/dt.

“[Silicate polymerization] occurs slowly at standard room temperature, but it can be greatly accelerated by curing at elevated temperature and it may be induced also by drying.”

Fairbairn et al. 2004:

Faria et al 2006:

Garner and Hammons 1991:

Graybeal 2006:

Graybeal 2011:

UHPC has greatly improved mechanical properties and porosity that makes it incredibly durable and rugged when compared to conventional concrete.

Increased strength in both compression and tension allow for structural components to be optimized and redesigned.

UHPC can be used in construction joints of precast section as an effective grouting material.

More issues with mixing and curing than regular concrete.

Curing at high temperature increases strength.

Green et al. 2015:

USACE ERDC has been researching UHPC for over 30 years.

UHPC is a concrete mixture with very low w/c, fc > 30ksi, low porosity, and dispersed steel fibers.

Optimization of material constituents lead to the Cor-Tuf and Cor-Tuf Baseline mixtures.

Although more expensive than conventional concrete, improved durability and strength can outweigh the cost when performance is needed.

Habel et al. 2006:

This study only looks at the CEMTEC-multiscale brand of UHPC cured at 100% RH and 20°C.

This paper presents a study to develop a time dependent mechanical model that can evaluate the potential of cracking.

It has been shown that the development of concrete’s mechanical properties is not a function of reaction rate, but degree of hydration indices such as maturity, equivalent time, or degree of hydration.  ISOTHERMAL AT 20°C

Evaluated compressive strength, elastic modulus, tensile strength, tensile modulus, linear-free and restrained autogenous shrinkage, and hardening as a function of DRI using power function curve. Correlation coefficients of 0.72 to 0.94!  ALSO ISOTHERMAL AT 20°C

Final degree of hydration achieved was only 0.31 due to the self-desiccating property of UHPC that completely consumes capillary water.  BTW, ISOTHERMAL AT 20°C

Hydration reaction is virtually complete by 90 days (99%) compared to the years or decades it can take for conventional concrete.  DID I NOT SAY THIS STUDY WAS ISOTHERMAL AT 20°C

Tensile properties develop more slowly than compressive properties.

Kodur et al. 2016:

Finite element model that traces temperature development. Referenced thermal properties of UHPC blend. Mechanical property model adopted by Maruyama et al. 2012.

Comparison of calculated thermal stress development to time-dependent strength properties NOT TEMPERATURE!

Parameteric studies were conducted to predict the effect of batch mix proportions, size of the concrete block, effect of insulation, and effect on reinforcement have on the development of heat, strength, and stress.

Numerical results showed that insulation can slow the rate of heat dissipation and reduce the thermal gradient and consequently reduce the likelihood of crack development.

Kuriakose et al. 2016:

Lawrence et al. 2012:

Focus on conventional concrete with different proportions of cement, GGBFS, and Class F Fly ash to evaluate the maximum allowable temperature gradient, but w/c is 0.5.

“Rate of mechanical strength development and thermal stress development are functions of material properties and temperature.”

Experiments on 4, 1 m3 blocks were compared to finite element predictions

Maruyama et al. 2012:

PCA 1997:

Heat of Hydration of cement is an important design consideration for certain projects.

Nonlinear expansion can cause cracking as temperature gradients develop. Insulation has been used to limit the thermal gradient.

A maximum allowable temperature rise of 20°C is standard for construction specifications.

Heat of hydration depends on the type of cement.

Use of low heat cement, minimizing cement content, using pre-cooled mix ingredients or ice, decelerating admixture, and cooling pipes can be used to reduce heat development.

Ulm and Coussy 1995:

The cement hydration reaction can be described by thermodynamics of open porous media.

Diffusion of water through the layers of hydrates is considered as the dominant mechanism of hydration.

Big proponent of equivalent age for isothermal conditions.

A key hypothesis of Ulm and Coussy is that the stress and temperature variations do not effect the thermodynamic imbalance between chemical constituents of the hydration reaction, than an “equivalent age” (or “maturity”) may be defined as an equivalent thermodynamic state variable describing the “aging” of the material.  BUT WHAT IF THERE BECOMES AN IMBALANCE: C-O-H precipitation, silica fume affinity based on temperature, thermally induced micro-cracking of cement matrix at intermediate ages.

Wan et al. 2016:

UHPC! Silica fume allows a pozzolanic reaction to produce additions calcium-silicate-hydrate (C-S-H) which can fill the would-have-been voids and provide a much denser matrix.

They include the silica fume reaction in their material model.

They performed experimental tests with curing room and SC (equivalent) specimens.

“Being able to model how the material ages and at what pace each mechanical property grows could greatly help optimize the construction sequence and hereby reduce the total construction time and budget.”

The behavior at early age is also of relevance for the long-term performance and durability due to restrain forces, cracking at early age. A computation framework is quintessential to the accurate performance assessments

Characterization of complex early age behavior is critical to accurate performance assessment and necessitates a computation framework that considers many material and environmental parameters.

Modeling of UHPC with the lattice discrete particle model (LPDM) which can consider the following nonlinear mesoscale phenomena: 1)fracture and cohesion, 2) compaction and pore collapse, and 3) friction.

Kim et al. 1998:

Subjected cured at constant temperatures of 5°C, 20°C, and 40°C bath curing. Specimens were also cured at variable temperatures in which the temperature starts at 20°C changes to either 5°C or 40°C or a day at a prescribed time, and returned to 20°C. The variable temperature curing was conducted to evaluate and modify the reaction rate constant.

The materials tested showed the cross-over behavior!

Kim et al. 2001:

Models the apparent activation as a nonlinear function of temperature and age.

They use the hyperbolic equation for the strength function and reaction.

Arrhenius and Saul temperature function did not predict strength based on curing temperatures very accurately using a constant activation energy  adjustment to correct maturity!

Lee et al. 2016:

They look at developing a strength model for high early strength concrete at different curing temperatures. They show the cross-over effect!

Our function is very similar! They had to correct it with a few factors.

Newbolds et al. 2001:

They demonstrated a good correlation between maturity development of cement paste and the degree of hydration of cement.

Air cured specimens did not produce as high of strength compared to those in a lime-bath.

Sbia et al. 2017:

Ready-mix concrete plant produced UHPC and made a reinforced 3.3’x3.3’x3.3’ cube with insulation that cured itself! Achieved strength of 24.7 ksi.