Improved Understanding of Concrete Compressive Strength Utilizing Cement Paste Testing

Bradley S. Hansen, Jay Shannon, and Isaac L. Howard

ABSTRACT

This paper provides information for use of cement paste (mixture of water, cementitious materials, and possibly admixtures but no coarse or fine aggregates) compressive strength testing to improve understanding of concrete. Cement paste testing has potential value because test cylinders can be produced much more easily than concrete. Results from almost 5000 data points showed cement paste strength trends were linear with respect to water to cementitious ratio, especially at earlier test days. Cement paste variability was greater than concrete variability in some cases. Cement paste strengths at later ages were disproportionately stronger than concrete and became less useful. Cement paste helped diagnose behaviors seen in concrete. Portland-limestone cement paste strength was always greater than ordinary portland cement paste within a group of several cements. In some cases, cement paste results showed that concrete with portland-limestone cement performed better than ordinary portland cement due to a better paste system. In other cases, cement paste results were able to provide strong evidence that concrete with portland-limestone cement performed better due to paste aggregate bond improvements relative to ordinary portland cement mixtures. In a third set of cases, cement paste results showed portland-limestone cement improved paste strength, but this improvement did not translate to concrete strength.

Keywords

Cement Paste, Mixture Proportioning, Quality Control/Assurance, Supplementary Cementitious Materials, Paste Aggregate Bonding

Introduction

In recent years, there has been a progressive effort to improve concrete’s sustainability while maintaining key performance characteristics that have made this versatile material one of the most commonly used in existence. The cementitious matrix within concrete is one of the keys to sustainability and performance, and is also the component of concrete that has grown increasingly complex over the past several years. Modern concrete can contain virtually infinite combinations of ordinary portland cement (OPC) as defined in ASTM C150 [1], portland-limestone cement (PLC) as defined in ASTM C595 [2], slag cement as defined in ASTM C989 [3], fly ash (Class C or F) as defined in ASTM C618 [4], and a host of other ingredients. The importance of the cementitious matrix to performance (e.g. setting and strength gain), make this a timely study when simultaneously considered alongside: 1) the complexity just exampled and; 2) the sustainability implications of the cementitious materials chosen.

Over the past ten to fifteen years, cement paste (CP) cylinders have been studied by a group of investigators from Holcim (US), now LafargeHolcim referred to hereafter as (LH), and Mississippi State University (MSU); see [5-16]. CP contains cementitious materials, water, and sometimes admixtures (no coarse or fine aggregates are included). CP in is usually formed into 5.1 cm diameter by 10.2 cm tall cylinders for subsequent measurements. As described in the next section, CP testing originated within the aforementioned LH research efforts to measure thermal profiles at very early ages, with some secondary compressive strength testing of the hardened paste cylinders produced. The recently released ASTM C1753 [17] is a product where the work of LH (Tim Cost and colleagues [5-11]) were key resources. ASTM C1753 focuses on use of CP for thermal measurements, that are sometimes supported by compressive strength measurements on the same cylinders where thermal measurements were taken (usually at 1 day (D)).

In more recent efforts, the MSU group has extended compressive strength testing of cement paste cylinders from 1 to 180 days, and it is this data that is the focus of this paper. There is not a current standard for testing cement paste strength of cylinders. ASTM C109 [18] concerns mortar (fine aggregates are present) where mortar strength measurements are on cubes. The primary objective of this paper is to provide information for use of cement paste compressive strength testing of cylinders for the purpose of improved understanding of concrete. To accomplish this objective, cement paste cylinder compressive strengths were first assessed to determine water to cement ratio trends and variability. Thereafter, CP was used to provide additional clarity to a variety of concrete mixtures produced with gravel and limestone aggregates and several cementitious combinations containing varying type and amount of supplementary cementitious materials (SCMs). In particular, cement paste testing was shown to help isolate the effects of stronger (or weaker) paste systems from the effects of paste-aggregate bond (PAB). CP was also helpful in providing more clarity in property improvements that have been previously documented in concrete [12-16,19-21] relative to PLC and OPC comparisons.

Cement paste testing has potential value because test cylinders can be produced much more easily than concrete with 20 to 30 different mixtures being easily producible in one day by one operator. Even modest information with this level of effort can be fruitful. Cement paste testing is shown later in this paper to have some value as a screening tool to down-select the best cementitious combinations with which to make trial concrete batches, or it can also be a diagnostic tool for concrete that performs differently (better or worse) than would have been expected. Cement paste testing is not envisioned to replace concrete testing for final decisions, but is believed to have some value in the aforementioned contexts.

Experimental Program

This paper used data acquired over a six year period (summer 2012 to summer 2018) at MSU that can be divided into three groups: 1) 158 concrete mixes (roughly 1,900 tested cylinders) previously used in various ways in several publications [12-16,19,20]; 2) roughly 1,000 cement paste cylinders previously used as shown in Table 1 [13,15,16]; and 3) roughly 2,000 cement paste cylinders tested for purposes of this paper to compliment the concrete and cement paste data already available from previous publications. All these experiments were performed on the same set of raw materials using protocols described in the remainder of this section.

MATERIALS

Twelve cements were included in this investigation: five were ASTM C150 [1] Type I or I/II OPCs, and seven were ASTM C595 [2] Type IL PLCs. The twelve cement IDs are as follows with cement type, limestone percent, and Blaine fineness in parentheses: A1 (OPC, 2.2%, 422 m2/kg), A2 (PLC, 8.8%, 522 m2/kg), C1 (OPC, 0.1%, 403 m2/kg), C2 (PLC, 8.5%, 549 m2/kg), C3 (PLC, 10.3%, 482 m2/kg), C4 (OPC, 0.4%, 424 m2/kg), C5 (PLC, 13.0%, 579 m2/kg), D1 (OPC, 0.3%, 421 m2/kg), D2 (PLC, 5.2%, 440 m2/kg), D3 (PLC, 14.0%, 556 m2/kg), E1 (OPC, 4.0%, 407 m2/kg), E2 (PLC, 15.7%, 681 m2/kg). Each cement is identified by a letter and a number. The letter symbolizes the specific source location (A1 and A2 are from the same source).

Three SCMs were used: ASTM C618 [4] Class C fly ash (denoted C ash or C), C618 [4] Class F fly ash (denoted F ash or F), and ASTM C989 [3] Grade 100 slag cement (denoted S). Three ASTM C494 [22] admixtures were utilized: Type A water reducer (2.0 oz./cwt), Type S slump retainer (5.0 oz./cwt), and Type F high range water reducer (6.0 oz./cwt). All concrete and cement paste used the same admixture dosage rates.

Four aggregates were used to produce concrete in conjunction with the cements, SCMs, and admixtures identified in the previous paragraphs. Aggregates were defined by ASTM C33 [23] and were: Size 57 rounded gravel (denoted GR), Size 57 limestone (denoted LS), Size 8 rounded gravel (denoted PG), and a coarse sand (denoted CS). Saturated surface dry bulk specific gravity (Gsb-ssd) and water absorption (Abs) for coarse aggregates were: GR (2.47, 3.2%), LS (2.73, 0.4%), and PG (2.46, 3.1%). The coarse sand Gsb-ssd, Abs, sand equivalency (SE), and fineness modulus (FM) were 2.61, 0.7%, 87, and 2.6.

TEST METHODS

Concrete was machine mixed at a water to cementitious (w/cm) ratio of 0.43, made into cylinders (10.2 by 20.3 cm), cured one day in the molds on a lab bench, and then placed in a 100% humidity curing room at 21 to 25 oC in accordance with ASTM C192 [24]. Concrete compressive strength (fc) testing occurred in triplicate at 7, 14, 28 and 56 days (D) as per ASTM C39 [25] with 70 durometer pad caps; average values were used herein. To denote GR and LS concrete compressive strengths, the symbols fc-GR and fc-LS are used when applicable. Concrete mixtures were tested for slump and air content in accordance with ASTM C143 [26] and C231 [27], respectively. For reference, concrete slumps ranged from 18 cm to 23 cm while air content ranged from 1.5-3.3%.

Cement paste (CP) cylinders were produced as shown in Fig. 1. Dry materials and water were batched separately after which admixture was introduced into the water and stirred to uniformity. The cementitious materials were placed into a mixing bowl and the water-admixture combination was then added. The paste cylinders were mixed at w/cm ratios of 0.40, 0.43, or 0.50 with a kitchen mixer for 30 seconds on low and then 30 seconds on high. After mixing, the paste was poured, using a funnel, into three 5.1 by 10.2 cm cylinders and covered with a plastic cap to limit evaporation (the molds were filled to roughly 9.6 cm deep for capping clearance). There was no consolidation necessary since the cement paste had adequate workability. The entire mixing process from water addition to capping took approximately 2.5 minutes. The method of mixing used herein yielded uniform cement paste. Other standard cement paste mixing methods are available (ASTM C305 [28] and ASTM C1738 [29]) but the original intention of mixing cement paste specimens with a kitchen mixer was to begin thermal measurements within minutes of water addition (ASTM C1753). This mixing method is allowed based on ASTM C1753 which states any adequate mixing method is acceptable.

After mixing, CP cylinders were either placed on a lab bench for one day or thermal profiles were measured over one day for purposes outside this paper. After one day, cylinders were either removed from their plastic mold and either tested immediately or placed into the same curing room as concrete specimens. Bleeding was not assessed, but when specimens were extruded no standing water was observed. Cement paste compressive strength (fcp) was measured in triplicate using 70 durometer pad caps after 1, 7, 14, 28, 56, and 180D for most testing. In six cases 30 replicate specimens were produced with otherwise identical protocols for variability assessment (denoted V1-V6).

Results

Tables 2 through 5 contain all data used herein, which is explained progressively throughout this section. These tables contain 106 cementitious material combinations that led to 158 concrete mixes with two coarse aggregate types (GR and LS). The 106 cementitious combinations have been sorted into eighteen groups (A to R) where the only variable within a group is the cement used. Each combination was also given a mix ID interpreted as follows: Mix 13 has 60% of cement A1, 0% slag cement (S), and 40% Class C fly ash (C). The data in these tables encompass pure cement systems (i.e. no SCMs), binary systems (i.e. one cement and one SCM), ternary systems (i.e. one cement and two SCMs), and have cement replacement levels ranging from 40 to 70%.

A total of 3042 cement paste cylinders and 1893 concrete cylinders were tested to produce Tables 2 to 5 (all numbers except V1-V6 are the average of three specimens). All of this concrete data, and roughly 1/3rd of this cement paste data has been used in previous publications [12-16,19,20], which are highlighted as appropriate to reinforce points pertinent to this paper. There is data from the previous referenced documents excluded from Tables 2 through 5 to maintain consistency for this data set. The cement paste data collected with the raw materials remaining from [12-16,19,20] first added a considerable amount of cement paste at a 0.50 w/cm to compliment the roughly 1,000 cylinders already made at this w/cm ratio, and then used the remaining materials to assess 0.40 and 0.43 w/cm ratios and variability data sets as they had not been previously explored. Superscripts V1-V6 in Tables 2-4 indicate a variability set of 30 replicate specimens were tested. Mean and coefficient of variation (COV) are shown in table notes.

The primary advantage of this data set is having roughly 4,900 compressive strengths from 106 cementitious combinations. The primary disadvantage is this was not a designed experiment to assess cement paste; rather the data available and raw materials leftover were used to compile as comprehensive of a data set as possible. As such, points made throughout rely on select portions of the data provided in Tables 2 through 5.

CEMENT PASTE OVERALL TRENDS

Water to Cementitious Ratio Relationships

The first trend investigated was linearity of CP strength between different w/cm ratios. Linear regression was conducted for 24 cases where 7D-56D data was available for all three w/cm ratios. Fig. 2a displays a Coefficient of Determination (R2) frequency histogram containing the distribution of R2 values for all 96 linear regression cases (i.e. one regression per day for 24 mixes). At early ages (7 to 14D) R2 values indicate strong linearity. At 28D linearity is still strong with two points causing a lower R2. If these points are removed the 28D average R2 is 0.86. At 56D the variability of fcp testing is most likely decreasing in correlation for reasons explained later in this paper. For all 96 cases, the R2 was greater than 0.90 65% of the time and greater than 0.80 74% of the time. Fig. 2a provided enough evidence to conclude CP strength with w/cm ratio was reasonably linear in the range of w/cm ratios investigated. Thereafter, missing data for 0.43 w/cm CP in Table 5 was linearly interpolated between collected 0.40 and 0.50 w/cm CP data per day and shown in Table 5. The linearity found in Fig. 2a corresponds almost identically to the longstanding relationship Abram’s law (equation 1). The fit coefficients A and B were determined from the w/cm and the measured compressive strength values. The R2 was calculated based off the measured versus predicted values and the average R2 were within 0.02 of the linearly interpolation R2 values for each day as seen in Fig. 2b.

fcp= ABw/cm										      Equation 1

Cement Paste Strength Variability

Coefficient of variation (COV) values of the six Table 2 to 4 sets of thirty cement paste specimens were 4.7, 6.1, 8.8, 11.5, 19.2, and 26.6%. According to ACI 214R-11 Table 4.4 [30], lab trial batch concrete COV is classified as fair or better if below 7.0%. It is also noted in [30] that the variation of 10.2 by 20.3 cm concrete specimens is generally higher than the 15.3 by 30.6 cm concrete specimens used to generate the ACI tables. These variability differences may be due to size effects, which would imply even higher variability could be present if specimen size were reduced further. A small investigation of 15 cement paste cylinders (5 specimens each of sizes 10.2 by 20.3cm, 7.6 by 15.2 cm, and 5.1 by 10.2 cm) was conducted to assess potential size effects. The average and COV for this data was as follows: 27.0 MPa and 5.4% (5.1 by 10.2 cm), 27.1 and 6.0% (7.6 by 15.2 cm), 30.0 MPa and 2.7% (10.2 by 20.3 cm). The results indicated smaller sizes did have higher COVs, but there were not enough differences to conclusively claim that size significantly affected variability. Some improvements on specimen fabrication are being explored for future work, but these results are outside the scope of this paper. As produced herein, cement paste variability exceeded typically expected concrete variability in some cases.

Overall Relationships Between Cement Paste and Concrete

Fig. 3 plots global trends comparing 0.50 w/cm CP to 0.43 w/cm concrete. Fig. 3 employs linear regression through the origin (RTO), as do Fig 4. and Fig 5. In that linear RTO is relied upon heavily in this paper, and has a few attributes of pertinence to this paper, the remainder of this paragraph describes the technique before interpreting Fig. 3. When using linear RTO, the resulting R2 is not a true coefficient of determination because the regression was forced through the origin. In other words, the model forces there to be no intercept and with that being the case, R2 can actually range from -1 to 1.  A negative R2 as used herein is interpreted as having no meaningful correlation, and any of the R2 values should only be interpreted in a relative sense versus other R2 values in this manuscript. R2 values from linear RTO are not for comparison to R2 values from models that include an intercept. Several research studies have made effective use of linear RTO (e.g. [31-33]), and [34] provides a detailed statistical assessment of linear RTO.

Trends of CP and concrete with different w/cm are expected to be similar since CP acts linearly with respect to w/cm. Cement paste compressive strengths track with LS and GR concrete with comparabe R2 values in all cases; linear relationships were used in Fig. 3. If a power curve had been used instead to describe Fig. 3a-b the equations would be 0.41x1.28 and 0.23x1.35, respectively, with R2 of 0.83 and 0.80. All three plots have considerable scatter, which reinforces the point that CP is not intended to predict concrete strength, rather it is a tool to assess general behaviors of concrete which can provide useful information. A key observation is fcp values begin to increase at faster rates than gravel concrete (fc-GR) values at around 25 MPa and limestone concrete (fc-LS) values at around 40 MPa.  This suggests that as strengths increase at later ages, cement paste becomes progressively less useful for predicting concrete behavior. This behavior could be due to the bonding capabilities of different aggregates (i.e. crushed vs. rounded). In addition, cement paste strength gain does not substantially slow at the same time as concrete strength gain does. As such, there is less of a reason to explore cement paste strength after concrete strength gain considerablly slows. Practical limitations occur at later ages for cement paste testing as well. These limitations are discussed in the next paragraph.

ASTM C1231 [35] reports an unbonded capping strength threshold of 80 MPa for the 70 durometer neoprene caps used herein. Cement paste strengths exeeded this limit at 180D, 27, 10, and 63% of the time at w/cm levels of 0.50, 0.43, and 0.40, repectively. At 56D, the CP strength exceeded this limit 5, 11, and 57% of the time at w/cm levels of 0.50, 0.43, and 0.40, respectively. At 28D, the limit was exceeded 0, 0, and 14% of the time at w/cm levels of 0.50, 0.43, and 0.40, respectively. At 14D and earlier, no cement paste specimens exceeded 80 MPa. Thus, CP testing at 180D provided no data to suggest there was enough value in the measurements to explore alternative capping (or other) systems, while testing at 56D may also prove to be unproductive. The main reason for the lack of value is the large variability at later age testing coupled with incapability of using 70 durometer neoprene pad caps. Testing cement paste cylinders with pad caps is for simplicity so alterantive capping or grinding methods are, in the authors opinion, in contrast to the goals and purpose of cement paste strength testing. Additionally, as mentioned in the previous paragraph there is minimal benefit to testing cement paste past the point that concrete strength gain substantially slows for purposes such as those described in this paper.

Fig. 3 incorporated all sources and mix proportions. Additional plots were made which were omitted for brevity where each cement source was assessed individually in the same manner as Fig. 3. For fc-GR versus fcp (comparable to Fig. 3a), cement source regression through origin (RTO) slopes ranged from 1.11-1.27 and R2 ranged from 0.69-0.75. For fc-LS versus fcp (comparable to Fig. 3b) cement source slopes ranged from 0.86-0.98 and R2 ranged form 0.63-0.77. Concrete (comparable to Fig. 3c) cement source slopes ranged from 1.14-1.32 and R2 ranged from 0.73-0.85. If individual cement sources were investigated or if all data was assessed collectively, observations were the same. With such a wide range of materials, an R2 in these ranges is believed by the authors to be promising.

CEMENT PASTE RELATIONSHIPS ACROSS PRODUCTION FACILITIES

This section interprets four pairs of cements, one OPC and one PLC from each of the four cement plants investigated. These 8 cements were those primarily assessed as pairs in [12-16,19,20]. Pairing these cements allowed systematic investigation of OPC to PLC differences from the same cement plant where information from CP was the focus.

Relationships at Different Water to Cementitious Ratios-Multiple Facilities

Fig. 4 shows OPC strength versus PLC strength for fc-GR, fc-LS, and fcp. The group identifier (e.g. A, B) corresponds to Table 2-4 so plots vary only by cement source and are paired. Equality plots were used that have the same axis with a line of equality (slope of 1) bisecting the graph. The data for equality plots is an ordered pair of similar data. When assessed with linear RTO, equality plots can show variable favorability. For example, in Fig. 4 an RTO slope of 1.43 indicates PLC strengths are higher than OPC strengths by approximately 43%. Two-tailed paired t-tests were conducted at a significance level of 0.05 to compliment Fig. 4. Variable 1, variable 2, average mean difference (AMD), and p-value are given in Table 6. Each case denotes the concrete mix type (GR or LS), or CP as well as the 2 variables of interest. Contents of Fig. 4 and Table 6 are discussed concurrently.

Fig. 4 shows that group A mixtures for OPC and PLC have similar strengths, but CP strength appeared to show slight PLC favorability. Cases 1, 6, and 13 confirmed that group A (100% cement) mixtures are not statistically different when comparing OPC and PLC. Relative to group A, slopes increased considerably by 0.42, 0.20, and 0.25 for fc-GR, fc-LS, and fcp, respectively. A similar increase in slopes between CP and LS concrete indicate a better cement paste system with PLC than OPC, but provides no evidence of paste aggregate bond (PAB) concerns. The change in GR concrete’s slope from group A to B was approximately double the change in CP’s slope from group A to B. This does indicate potential PAB problems with C ash and GR concrete with OPC as first mentioned in [13]. The data considered herein excludes 1D and 180D whereas [13] considered 1D to 180D data. Group B PAB issues seem to be mitigated by PLC. These behaviors can be quantified by the AMD of case 20 and 21 of 15.3 MPa and 3.8 MPa, respectively. Although both are statistically different, the AMD shows that PLC was able to better sustain fc-GR relative to 100% cement (only lost 3.8 MPa) while the OPC strengths dropped substantially relative to 100% cement (lost 15.3 MPa). Absent cement paste data, mechanisms for PLC’s superior performance would not be as easily assessed.

The ternary case of group H shows the same slope change of +0.11 relative to group A for LS concrete, GR concrete, and CP which suggests increases are attributable to a better cement paste system. Group H also showed a consistent benefit of PLC relative to OPC in concrete and paste. The paste in this case indicates PLC makes a better cementitious system while PAB remained seemingly unaffected. Group B (40% C ash) and group H (30% slag cement and 20% C ash) showed statistical differences with PLC always being higher than OPC (cases 2, 3, 7, 9, 14, and 16) which validates PLC synergies with C ash. At 70% replacement, the CP slope in Group Q was well above 1.0 indicating PLC performed better. However, neither concrete saw benefit with PLC possibly implying cement paste testing identified PAB issues as first noted in [19]. At 70% replacement, Cases 5, 11, and 18 validated no significant strength benefit from PLC in group Q with concretes, but CP showed substantial benefit with an AMD of -12.5 MPa indicating much higher PLC strengths.

When 40% F ash mixtures are used (group C) the synergies between C ash and PLC are apparent relative to concrete [see 20 for more information]. CP and limestone concrete in group C show similar slopes to group A which would imply little benefit with PLC and F ash relative to bonding for the data presented. The synergies between C ash and PLC are further highlighted when comparing similar mixture combinations of class F and C fly ash. Cases 4, 8, 10, and 12 show there is not a statistically significant difference in concrete using F ash with PLC. Cement paste with F ash (cases 15, 17, and 19) showed statistically significant benefit of PLC with F ash, but Fig. 4 shows this did not translate to concrete. By looking at the AMDs between C ash and F ash mixtures, the PLC synergies with C ash are easily observed as discussed in the next paragraph.

In groups C, I, and R (F ash mixtures), CP slopes ranged from 1.05-1.07 while groups B, H, and Q (C ash mixtures) ranged from 1.16-1.30. This indicates CP with C ash showed synergies with PLC while F ash did not. In cases 22-25, LS and CP mixtures with C ash and F ash were compared.  Case 22, 24, and 25 all showed statistically different benefit with C ash while only case 23 showed F ash to have statistically improved strength with an AMD of -6.9. When CP strength does not benefit from PLC, this suggests the concrete would not benefit either, provided PAB effects are not present (groups C, I, and R) which is reinforced by Fig. 4. Conversely, when CP strength increases with PLC and the concrete strengths do not, then this implies potential PAB issues (group Q). Concrete in groups B and H show benefit from PLC while group Q does not, as first reported in [13,16,20].  Overall this indicates CP tracked well with concrete at replacement rates up to 50%.

Relationships at a Constant Water to Cementitious Ratio-Multiple Facilities

Fig. 5 compares all available data for 0.43 w/cm ratio concrete (GR and LS) where a CP pair from the 8 cements described to begin this section existed. The AMD and p-value are given in Fig. 5 for reference. The two global plots show that CP at the same w/cm ratio, overall, is 51% stronger and 21% stronger than GR and LS concrete, respectively. CP tracks with concrete to some degree, but the data has scatter, especially at later ages. When dividing the global plot into test day, obvious trends emerge. First, the R2 progressively drops as age increases. This indicates that paste testing tracks better at early ages. Second, in almost all cases, CP is stronger than concrete. The CP data which is weaker can typically be attributed to testing variability. This means CP strength could be treated as an upper limit of possible concrete strengths for traditional ready mixed proportions and materials. For example, if the CP strength is 32 MPa and the concrete is 27 MPa (Mix 50 at 14D), then there is no reason to believe the concrete has any bonding problems. Conversely, if concrete strength is much lower than CP strength (e.g. 34 MPa vs. 61 MPa (Mix 3 at 14D), the producer has opportunities to change aggregates, admixtures, gradation, or other to derive more value from the cementitious system of interest.

To provide visual examples of how cement paste can aid concrete proportions decision making, bar charts were constructed of four example cases (Fig. 6). Twenty-three mixtures from groups A, H, and Q for 4 different cement source OPC and PLC pairs (previously identified in [13,20]) were categorized into these four cases: 1) Similar concrete and CP strengths; 2) CP strength is much higher than concrete strength; 3) one aggregate produces substantially higher concrete strengths; 4) a combination of cases 2 and 3. Of the 23 mixes considered, 8 were case 1, 4 were case 2, 5 were case 3, and 5 were case 4. A producer could improve concrete decision making by assessing their products in this manner, which is made possible by cement paste data. For example, case 2 mixtures could benefit from a completely new aggregate or a change to a different cement system which shows better bonding. Case 3 mixtures could help choose a more appropriate aggregate for a given cement system. If a mixture is classified case 4, then both steps taken in case 2 and 3 should be investigated with a higher probability of a trial and error process. Case 1 mixtures have similar CP, GR concrete, and LS concrete strengths which indicate decisions could be based on cost and material availability with any improvements requiring a better cementitious system as CP strength has shown to be an upper limit for concrete strengths.

CEMENT PASTE TRENDS FROM ONE FACILITY

An investigation into only one cement source, source C, was conducted since 5 cements were available (C1-C5) to see if findings already reported still hold. Cement source C followed the global trends with respect to concrete versus CP strengths already presented. The RTO slopes for GR and LS concrete versus 0.50 w/cm paste with source C were 1.21 and 0.94, respectively. These numbers were essentially the same when all data was considered in Fig. 3. Additional plots were made to investigate cement source C, but the authors found no new information to suggest different assessments from previous sections.

Summary and Conclusions

Approximately 1900 concrete and 3000 cement paste cylinders were used in this paper to assess cement paste (CP) behavior relative to concrete. CP generally followed similar trends which have been observed in concrete. Cement paste compressive strengths have shown additional value than has been previously derived from literature known to the authors. Observed CP behaviors are as follows:

- CP w/cm ratio compressive strength trends were linear especially at earlier test days.

- CP variability was generally greater than typical concrete variability.

- CP at later ages is disproportionately stronger than traditional ready mixed concrete; 180 day cured CP strength is not believed to be especially useful.

- CP was able to help diagnose behaviors seen in concrete such as paste aggregate bond and concrete property improvements due to improved paste properties. Four example cases were proved to allow a user to diagnose manners through which they might be able to improve their concrete. Note that paste aggregate bond is an extremely complex behavior and that the authors are not claiming the methods used herein can fully capture these complexities. Rather, these methods can provide more information than would otherwise be available in this regard.

ACKNOWLEDGEMENTS

Thanks are due to the financial supporters of the Cement & Concrete Industries Excellence Fund, the member companies of the Mississippi Concrete Association, and especially to Tim Cost, F.ACI (LafargeHolcim-Retired) for his many years of support and guidance on cement paste testing.

References

[1] Standard Specification for Portland Cement, ASTM C150/C150M-18, (West Conshohocken, PA: ASTM International, April 1, 2018). https://doi.org/10.1520/C0150_C0150M-18.

[2] Standard Specification for Blended Hydraulic Cements, ASTM C595/C595M-18, (West Conshohocken, PA: ASTM International, April 1, 2018). https://doi.org/10.1520/C0595_C0595M-18.

[3] Standard Specification for Slag Cement for Use in Concrete and Mortars, ASTM C989/C989M-18, (West Conshohocken, PA: ASTM International, December 15, 2018). https://doi.org/10.1520/C0989_C0989M-18.

[4] Standard Specification for Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use in Concrete, ASTM C618-17a, (West Conshohocken, PA: ASTM International, December 15, 2017). https://doi.org/10.1520/C0618-17A.

[5] V. T. Cost and G. Knight, “Use of Thermal Measurements to Detect Potential Incompatibilities of Common Concrete Materials,” Concrete Heat Development: Monitoring, Prediction, and Management. ACI SP-241-4, Atlanta, GA, 2007, pp. 39-58.

[6] V. T. Cost, “Thermal Measurements of Hydrating Concrete Mixtures – A Useful Quality Control Tool for Concrete Producers,” NRMCA Publication 2PE004, National Ready Mixed Concrete Association, 900 Spring Street, Silver Spring, MD, August 2009, pp. 1-10.

[7] V. T. Cost, and A. Gardiner, “Practical Concrete Mixture Evaluation via Semi-Adiabatic Calorimetry,” (paper presentation, Concrete Technology Forum – Focus on Performance Prediction, Cincinnati, OH, month, May 15, 2009).

[8] V. T. Cost, “Concrete Sustainability versus Constructability – Closing the Gap,” (paper presentation, International Concrete Sustainability Conference, Boston, MA, August 9, 2011).

[9] V. T. Cost, “Preliminary Optimization of Concrete Paving Mixtures for Sustainability and Performance,” (paper presentation, Tenth International Conference on Concrete Pavements, Quebec City, Quebec, 2012).

[10] V. T. Cost and P. Bohme, “Synergies of Portland-Limestone Cements and Their Potential for Concrete Performance Enhancement,” (paper presentation, 2012 International Concrete Sustainability Conference, Seattle, WA, May 9, 2012).

[11] V. T. Cost, I.L. Howard, and J. Shannon, “Improving Concrete Sustainability and Performance with Use of Portland-Limestone Cement Synergies,” Transportation Research Record:  Journal of the Transportation Research Board, No. 2342 (2013): 26-34.

[12] V. T. Cost, T. Matschei, J. Shannon, and I.L. Howard, “Extending the Use of Fly Ash and Slag Cement in Concrete Through the use of Portland-Limestone Cement,” (paper presentation, 2014 International Concrete Sustainability Conference, Boston, MA, May 13, 2014).

[13] J. Shannon, I. L. Howard, V. T. Cost, and W.M. Wilson, “Benefits of Portland-Limestone Cement for Concrete with Rounded Gravel Aggregates and Higher Fly Ash Replacement Rates”. (paper presentation, 94th Annual Meeting of the Transportation Research Board, Washington, D.C., January, 2013).

[14] V.T. Cost, W. Wilson, J. Shannon, and I.L. Howard, “Unexpected Concrete Performance Benefits of Sustainable Binder Combinations Using Portland-Limestone Cement,” (paper presentation, Fifth International Conference on Construction Materials: Performance, Innovations and Structural Implications, Whistler, Canada, 2015.

[15] J. Shannon, “Performance and Sustainability Benefits of Concrete Containing Portland-Limestone Cement,” (PhD dissertation, Mississippi State University, 2015).

[16] J. Shannon, I. L. Howard, and V. T. Cost, “Potential of Portland-Limestone Cement to Improve Performance of Concrete Made with High Slag Cement and Fly Ash Replacement Rates,” Journal of Testing and Evaluation 45, No. 3 (May 2017): 873-889.

[17] Standard Practice for Evaluating Early Hydration of Hydraulic Cementitious Mixtures Using Thermal Measurements, ASTM C1753/C1753M-15e1, (West Conshohocken, PA: ASTM International, August 1, 2015). https://doi.org/10.1520/C1753_C1753M-15E01.

[18] Standard Test Method for Compressive Strength of Hydraulic Cement Mortars (Using 2-in. or [50-mm] Cube Specimens), ASTM C109/C109M-16a, (West Conshohocken, PA: ASTM International, March 1, 2016). https://doi.org/10.1520/C0109_C0109M-16A.

[19] I.L. Howard, J. Shannon, V.T. Cost, and M. Stovall, “Davis Wade Stadium Expansion and Renovation: Performance of Concrete Produced with Portland-Limestone Cement, Fly Ash, and Slag Cement,” Journal of Materials in Civil Engineering, 27, No. 12 (December 2015). https://doi.org/10.1061/(ASCE)MT.1943-5533.0001305.

[20] J. Shannon, I.L. Howard, V.T. Cost, and W. Crawley, “Synergistic Potential of Fly Ash in Concrete Featuring Portland-Limestone Cement,” ACI Materials Journal, 114, No. 2, (March 2018): 295-306.

[21] V.T. Cost, G. Knight, W. Wilson, J. Shannon, and I.L. Howard, “Performance of Typical Concrete Mixtures for Transportation Structures as Influenced by Portland-Limestone Cements from Five Sources,” (paper presentation, 2013 International Concrete Sustainability Conference, San Francisco, CA, May 7, 2013).

[22] Standard Specification for Chemical Admixtures for Concrete, ASTM C494/C494M-17, (, West Conshohocken, PA: ASTM International, June 15, 2017).

https://doi.org/10.1520/C0494_C0494M-17.

[23] Standard Specification for Concrete Aggregates, ASTM C33/C33M-18, (West Conshohocken, PA: ASTM International, March 15, 2018).

https://doi.org/10.1520/C0033_C0033M-18.

[24] Standard Practice for Making and Curing Concrete Test Specimens in the Laboratory, ASTM C192/C192M-16a (West Conshohocken, PA: ASTM International, June 1, 2016).

https://doi.org/10.1520/C0192_C0192M-16A.

[25] Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens, ASTM C39/C39M-18, (West Conshohocken, PA: ASTM International, January 1, 2018).

https://doi.org/10.1520/C0039_C0039M-18.

[26] Standard Test Method for Slump of Hydraulic-Cement Concrete, ASTM C143/C143M-15a, (West Conshohocken, PA: ASTM International, December 15, 2015).

https://doi.org/10.1520/C0143_C0143M-15A.

[27] Standard Test Method for Air Content of Freshly Mixed Concrete by the Pressure Method, ASTM C231/C231M-17a, (West Conshohocken, PA: ASTM International, April 15, 2017). https://doi.org/10.1520/C0231_C0231M-17A.

[28] Standard Practice for Mechanical Mixing of Hydraulic Cement Pastes and Mortars of Plastic Consistency, ASTM C305-14, (West Conshohocken, PA: ASTM International, August 1, 2014). https://doi.org/10.1520/C0305-14.

[29] Standard Practice for High-Shear Mixing of Hydraulic Cement Pastes, ASTM C1738/C1738M-18, (West Conshohocken, PA: ASTM International, May 1, 2018).

https://doi.org/10.1520/C1738_C1738M-18.

[30] ACI Committee 214, “Guide to Evaluation of Strength Test Results of Concrete,” ACI 214R-11. American Concrete Institute, (April 2011): 7.

[31] F. Vahedifard, I.L. Howard, W.H. Badran, W.D. Carruth, M. Hamlehdari, and B.D. Jordan, “Strength Indices of High-moisture Soils using Handheld Gauges,” Institution of Civil Engineers-Ground Improvement, 169(GI3), (August 2016): 167-181.

[32] I.L. Howard and W.D. Carruth, “Dewatering and Stabilizing Fine-Grained Soils with Very High Moisture Content,” Advances in Civil Engineering Materials, 3, No. 1, (March 2014): 220-237.

[33] W.D. Carruth and I.L. Howard, “Use of Portland Cement and Polymer Fibers to Stabilize Very High Moisture Content Fine-Grained Soils,” Advances in Civil Engineering Materials, 2, No. 1, (February 2013): 1-24.

[34] Eisenhower, J.G., “Regression Through the Origin,” Teaching Statistics, 25, No. 3, (2003): 76-80.

[35] Standard Practice for Use of Unbonded Caps in Determination of Compressive Strength of Hardened Cylindrical Concrete Specimens, ASTM C1231/C1231M-15, (West Conshohocken, PA: ASTM International, December 1, 2015). https://doi.org/10.1520/C1231_C1231M-15.

List of Tables

Table 1 - Cement Paste Literature Review

Table 2 - Cement Paste and Concrete Compressive Strengths (Mixes 1-32)

Table 3 - Cement Paste and Concrete Compressive Strengths (Mixes 33-68)

Table 4 - Cement Paste and Concrete Compressive Strengths (Mixes 69-106)

Table 5 - Cement Paste Compressive Strengths with Varying Water to Cementitious Ratios

Table 6 - t-test Results Relative to Fig. 4

TABLE 1 Cement Paste Literature Review

| Reference | Variables of Interest | Thermal Testing | Paste Strength | Key Findings |
| --- | --- | --- | --- | --- |
| [5] Cost and Knight (2007) | Mix incompatibility | Yes | None | Sulfate balance is vital for performance. Sulfate issues can arise in high replacements of Class C fly ash, hot weather, and from admixtures. Thermal measurements can quickly test mix sensitivities. |
| [6] Cost (2009) | Mix incompatibility | Yes | None | Thermal measurements are an effective diagnostic tool to show hydration differences of CP mixture variables. Results can generally predict concrete behavior. |
| [7] Cost and Gardiner (2009) | Setting time | Yes | Yes 1D | Concrete, mortar, and paste can all be used with thermal measurements to assess mix performance. Concrete and mortar can be directly related to ASTM C403. Paste thermal set was approximately 141-151% of ASTM C403 initial set time. CP Thermal profiles can denote mix incompatibility. |
| [8] Cost (2011) | Admixtures, SCMs, and field testing | Yes | Yes 1D | Cement clinker factors can be reduced making concrete more sustainable with usage of thermal measurements and 1 day CP strength to investigate compatibility of aggressive admixture use as well as high SCM replacements. The process can ensure proper setting and strength gain. |
| [9] Cost (2012) | Mixture optimization | Yes | Yes 1D-7D | Thermal measurements provide a faster way to develop mixture quantities of admixture, cement, and SCMs by getting relative performance indicators from only CP thermal profiles and strengths. Thermal setting times for CP mixtures are longer than C403 setting, but follow concrete trends. |
| [10] Cost and Bohme (2012) | Portland-limestone cement | Yes | Yes 1D-7D | Limestone additions can reduce clinker factors and enhance setting and increase strength. With a Blaine’s fineness increase of 100 m2/kg, PLC shows equivalent or better performance than OPC. |
| [11] Cost et al. (2013) | Portland-limestone cement | Yes | None | CP was used alongside concrete to show enhancement potential of PLC is dependent on limestone fineness. Strength and setting performance was increased at 10% limestone as limestone fineness increased. Coarser limestone caused set retardation in Class C ash. Setting continued to accelerate at 15% limestone, but strength remained unchanged relative to 10% limestone. PLC showed physical and chemical interaction synergies with SCMs based on limestone fineness. |
| [12] Cost et al. (2014) | Portland-limestone cement | Yes | Yes 1D-28D | CP from one cement source indicated higher than normal SCM levels is possible with PLC in place of OPC with equivalent strength performance, especially with Class C fly ash and slag blends. |
| [13] Shannon et al. (2015) | Portland-limestone cement | Yes | Yes 1D-180D | PLC with 40% Class C fly ash had higher strengths than similar OPC mixtures in concrete and CP. Concrete and CP with slag showed PLC benefits at 7 days but less benefit at later ages. Paste aggregate bond (PAB) appeared to be better in all cases with slag relative to fly ash. The authors noted differences between concrete and CP trends could be due to differences in PAB. Petrography showed differences in CP and the interfacial transition zone between OPC and PLC. |
| [14] Cost et al. (2015) | Portland-limestone cement | No | Previous work | Smooth gravel aggregate strength issues with fly ash could be mitigated by PLC use in place of OPC. Authors note paste aggregate bond improvement with PLC based on CP and lab concrete. |
| [15] Shannon (2015) | Portland-limestone cement | Yes | Yes 1D-180D | PLC is equal or better than OPC (mostly) especially with SCMs. Dissertation where 2280 concrete and 2388 CP cylinders were collected (only 1560 concrete and 1047 CP cylinders were used). |
| [16] Shannon et al. (2017) | Portland-limestone cement | No | Yes 1D-56D | For CP all SCM combinations had higher strengths with PLC relative to OPC for cases up to 50MPa. Between 50-70MPa CP strength performance varied based on replacement rate. CP at 50% cement showed considerably higher strengths with PLC for 50-70MPa, but higher replacements sometimes favored OPC. Early age CP PLC trended higher than OPC but at late ages strengths converged. PAB problems reported at 70% replacement based on CP and concrete. |

TABLE 2 Cement Paste and Concrete Compressive Strengths (Mixes 1-32)

| Group | Mix No. | Mix ID | Cement Paste fcp w/cm = 0.50 |  |  |  |  |  | Concrete fc w/cm = 0.43 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1D | 7D | 14D | 28D | 56D | 180D | 7D | 14D | 28D | 56D |
| A | 1 | 100C1/0S/0C | 12.6V1 | 36.9V2 | 49.8 | 57.0V3,4 | 59.8 | 57.2 | (36.8) [37.9] | (45.3) [44.5] | (49.6) [49.0] | (53.9) [55.1] |
|  | 2 | 100C3/0S/0C | 13.7 | 39.2 | 46.4 | 51.1 | 61.6 | 72.5 | (28.4) [---] | (32.6) [---] | (39.2) [---] | (41.8) [---] |
|  | 3 | 100C4/0S/0C | 12.6 | 39.4 | 46.3 | 59.2 | 67.2 | 68.8 | (30.1) [---] | (34.1) [---] | (39.0) [---] | (44.6) [---] |
|  | 4 | 100A1/0S/0C | 15.3 | 37.8 | 37.5 | 48.0 | 48.6 | 51.2 | (37.1) [42.9] | (42.8) [51.2] | (46.3) [54.1] | (49.3) [57.2] |
|  | 5 | 100D1/0S/0C | 14.6 | 34.0 | 43.0 | 48.9 | 54.1 | 63.4 | (35.3) [43.0] | (40.3) [45.5] | (43.2) [49.4] | (46.1) [54.0] |
|  | 6 | 100E1/0S/0C | 15.5 | 31.0 | 38.2 | 47.7 | 55.8 | 59.3 | (30.2) [40.4] | (35.1) [45.5] | (38.2) [50.1] | (40.4) [57.3] |
|  | 7 | 100A2/0S/0C | 19.6 | 32.6 | 34.2 | 37.0 | 37.1 | 41.3 | (33.3) [40.9] | (38.5) [44.1] | (42.7) [47.6] | (45.9) [54.8] |
|  | 8 | 100C2/0S/0C | 18.3 | 36.2 | 61.1 | 60.5 | 69.6 | 68.3 | (41.8) [39.3] | (48.0) [44.3] | (50.8) [46.8] | (52.2) [52.3] |
|  | 9 | 100C5/0S/0C | 17.9 | 36.9 | 47.0 | 49.2 | 53.7 | --- | (39.2) [39.8] | (43.9) [42.8] | (47.7) [50.9] | (52.3) [53.6] |
|  | 10 | 100D2/0S/0C | 9.0 | 27.8 | 39.5 | 46.3 | 51.9 | 52.7 | (36.4) [39.0] | (42.0) [39.8] | (46.3) [46.0] | (48.1) [52.8] |
|  | 11 | 100D3/0S/0C | 18.4 | 40.2 | 47.4 | 53.1 | 58.1 | 59.5 | (38.5) [41.5] | (41.5) [46.4] | (45.6) [49.7] | (50.2) [54.3] |
|  | 12 | 100E2/0S/0C | 21.2 | 42.3 | 46.2 | 55.0 | 52.6 | 59.8 | (31.6) [44.2] | (36.2) [50.5] | (38.5) [52.0] | (41.4) [59.7] |
| B | 13 | 60A1/0S/40C | 2.6 | 17.3 | 23.0 | 29.6 | 38.2 | 52.3 | (20.8) [24.6] | (25.1) [29.2] | (27.3) [38.2] | (35.7) [48.1] |
|  | 14 | 60C1/0S/40C | 1.4 | 14.0 | 21.1 | 29.5 | 48.6 | 57.8 | (19.8) [25.2] | (25.7) [30.9] | (30.0) [41.3] | (38.0) [51.5] |
|  | 15 | 60D1/0S/40C | 1.5 | 16.1 | 22.1 | 28.1 | 41.2 | 50.9 | (21.5) [34.6] | (24.5) [40.7] | (29.0) [45.5] | (33.1) [56.3] |
|  | 16 | 60E1/0S/40C | 2.7 | 16.1 | 22.2 | 30.2 | 45.3 | 59.4 | (17.1) [23.8] | (20.3) [32.7] | (27.1) [40.4] | (30.4) [50.3] |
|  | 17 | 60A2/0S/40C | 3.9 | 22.0 | 29.9 | 38.3 | 49.4 | 63.8 | (28.9) [32.4] | (33.7) [41.1] | (39.9) [45.4] | (42.5) [56.1] |
|  | 18 | 60C2/0S/40C | 2.8 | 26.1 | 35.5 | 44.2 | 49.9 | 60.9 | (29.6) [33.2] | (39.4) [42.4] | (43.1) [50.4] | (51.8) [62.2] |
|  | 19 | 60C5/0S/40C | 3.3 | 22.6 | 30.0 | 36.6 | 47.2 | 68.9 | (35.6) [29.6] | (41.6) [38.0] | (47.6) [44.9] | (56.0) [56.9] |
|  | 20 | 60D2/0S/40C | 0.4 | 19.0 | 26.8 | 32.5 | 37.7 | 54.3 | (26.1) [28.3] | (29.7) [35.0] | (34.1) [42.8] | (39.4) [50.4] |
|  | 21 | 60D3/0S/40C | 2.1 | 26.6 | 34.7 | 43.3 | 47.4 | 65.7 | (31.1) [31.8] | (35.1) [37.9] | (40.0) [46.5] | (41.3) [53.2] |
|  | 22 | 60E2/0S/40C | 5.5 | 26.3 | 35.2 | 43.6 | 52.6 | 67.4 | (32.0) [29.5] | (35.8) [36.5] | (43.5) [45.8] | (48.1) [52.0] |
| C | 23 | 60A1/0S/40F | 4.5 | 13.8 | 18.6 | 23.8 | 32.6 | 48.7 | (---) [22.7] | (---) [29.2] | (---) [36.2] | (---) [44.0] |
|  | 24 | 60C1/0S/40F | 2.5 | 8.9 | 14.5 | 23.3 | 33.0 | 43.8 | (---) [20.2] | (---) [27.4] | (---) [34.0] | (---) [43.1] |
|  | 25 | 60D1/0S/40F | 3.8 | 11.3 | 16.5 | 23.4 | 28.9 | 48.5 | (---) [26.9] | (---) [34.6] | (---) [38.4] | (---) [46.3] |
|  | 26 | 60E1/0S/40F | 3.2 | 13.2 | 19.1 | 26.4 | 36.5 | 37.5 | (---) [17.7] | (---) [25.8] | (---) [31.3] | (---) [36.2] |
|  | 27 | 60A2/0S/40F | 4.5 | 15.6 | 20.4 | 25.9 | 35.8 | 53.3 | (---) [20.4] | (---) [25.6] | (---) [33.3] | (---) [38.9] |
|  | 28 | 60C2/0S/40F | 6.9 | --- | --- | --- | --- | --- | (---) [24.8] | (---) [32.0] | (---) [37.8] | (---) [46.7] |
|  | 29 | 60C5/0S/40F | 4.6 | 14.4 | 20.9 | 27.3 | 42.5 | 33.7 | (---) [20.1] | (---) [26.9] | (---) [33.1] | (---) [47.7] |
|  | 30 | 60D2/0S/40F | 1.9 | 14.1 | 18.8 | 27.0 | 37.3 | 53.3 | (---) [25.4] | (---) [33.2] | (---) [39.8] | (---) [47.7] |
|  | 31 | 60D3/0S/40F | 4.6 | 15.8 | 19.8 | 25.3 | 33.6 | 40.7 | (---) [17.8] | (---) [29.4] | (---) [34.9] | (---) [40.5] |
|  | 32 | 60E2/0S/40F | 5.7 | 13.1 | 21.1 | 25.0 | 34.7 | 53.4 | (---) [17.3] | (---) [24.2] | (---) [28.2] | (---) [32.3] |

Notes: 	(gravel concrete strengths) [limestone concrete strengths]	Mix ID: % cement and source/ % slag/ % Class C fly ash or Class F fly ash

Group letter indicates different cementitious mix proportions

V1: Mean = 15.7MPa, COV = 8.8%, V2: Mean = 33.9MPa, COV = 4.7%, V3: Mean = 50.3MPa, COV = 6.1% and V4: Mean = 58.5, COV = 11.5%

TABLE 3 Cement Paste and Concrete Compressive Strengths (Mixes 33-68)

| Group | Mix No. | Mix ID | Cement Paste fcp w/cm = 0.50 |  |  |  |  |  | Concrete fc w/cm = 0.43 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1D | 7D | 14D | 28D | 56D | 180D | 7 | 14 | 28 | 56 |
| D | 33 | 50C1/50S/0C | 2.2 | 12.3 | 33.0 | 61.1 | 67.3 | 70.3 | (17.5) [---] | (36.9) [---] | (44.9) [---] | (50.1) [---] |
|  | 34 | 50C2/50S/0C | 3.8 | 37.2 | 47.9 | 56.5 | 61.6 | 66.9 | (26.7) [---] | (38.8) [---] | (45.3) [---] | (47.8) [---] |
| E | 35 | 50C1/0S/50C | 1.0 | 9.5 | 12.8 | 17.8 | 34.7 | 50.0 | (13.7) [---] | (18.0) [---] | (22.4) [---] | (29.1) [---] |
|  | 36 | 50C2/0S/50C | 1.5 | 19.2 | 25.0 | 32.2 | 43.8 | 55.9 | (21.9) [---] | (27.1) [---] | (31.2) [---] | (38.5) [---] |
| F | 37 | 50C1/40S/10C | 2.3 | 18.0 | 33.1 | 52.5 | 61.4 | 83.1 | (20.9) [---] | (33.1) [---] | (39.0) [---] | (48.5) [---] |
|  | 38 | 50C2/40S/10C | 4.4 | 25.9 | 50.2 | 60.4 | 72.1 | 82.3 | (33.9) [---] | (44.5) [---] | (50.7) [---] | (53.4) [---] |
|  | 39 | 50C3/40S/10C | 3.6 | 23.7 | 46.1 | 67.0 | 84.1 | 91.6 | (30.8) [---] | (43.9) [---] | (48.7) [---] | (55.1) [---] |
|  | 40 | 50C4/40S/10C | 3.0 | 11.6 | 23.7 | 57.6 | 84.8 | 97.9 | (16.0) [---] | (27.5) [---] | (39.6) [---] | (44.8) [---] |
|  | 41 | 50C5/40S/10C | 6.9 | 29.1 | 43.3 | 56.9 | 64.5 | --- | (29.1) [---] | (37.5) [---] | (44.5) [---] | (49.3) [---] |
| G | 42 | 50C1/25S/25C | 2.4 | 12.3 | 18.7 | 41.2 | 61.6 | 76.7 | (16.9) [27.6] | (24.2) [35.5] | (31.7) [47.5] | (38.5) [60.2] |
|  | 43 | 50C2/25S/25C | 3.7 | 21.7 | 32.1 | 52.9 | 69.1 | 78.4 | (31.3) [34.0] | (40.4) [46.2] | (49.9) [59.8] | (55.9) [69.5] |
|  | 44 | 50C3/25S/25C | 2.6 | 18.2 | 29.6 | 44.9 | 65.7 | 88.3 | (22.1) [28.2] | (32.0) [42.9] | (42.4) [54.4] | (49.1) [69.5] |
|  | 45 | 50C4/25S/25C | 2.4 | 12.0 | 19.0 | 45.6 | 60.2 | 74.9 | (12.7) [20.1] | (24.5) [27.8] | (34.9) [43.0] | (51.4) [57.5 |
|  | 46 | 50C5/25S/25C | 4.1 | 26.5 | 33.0 | 47.1 | 69.2 | --- | (26.5) [---] | (32.3) [---] | (41.7) [---] | (46.4) [---] |
| H | 47 | 50C3/30S/20C | 2.8 | 20.6 | 36.2 | 60.7 | 76.9 | 95.1 | (25.2) [---] | (34.9) [---] | (47.7) [---] | (57.4) [---] |
|  | 48 | 50C4/30S/20C | 2.7 | 13.9 | 20.2 | 41.8 | 52.4 | 84.6 | (16.8) [---] | (23.9) [---] | (36.5) [---] | (43.8) [---] |
|  | 49 | 50A1/30S/20C | 2.5 | 15.2 | 26.7 | 45.8 | 66.8 | 89.0 | (19.5) [25.1] | (26.0) [35.7] | (36.7) [48.6] | (47.4) [59.8] |
|  | 50 | 50C1/30S/20C | 2.0 | 12.5 | 20.5 | 39.7V5 | 65.6 | 91.3 | (18.3) [20.0] | (27.0) [29.2] | (39.1) [43.8] | (46.9) [52.8] |
|  | 51 | 50D1/30S/20C | 2.0 | 20.0 | 33.3 | 53.5 | 64.0 | 82.1 | (18.0) [22.9] | (26.0) [33.6] | (37.1) [39.5] | (44.0) [45.7] |
|  | 52 | 50E1/30S/20C | 2.2 | 17.5 | 30.3 | 48.6 | 66.3 | 68.7 | (18.7) [23.6] | (28.1) [42.1] | (35.7) [53.6] | (44.4) [63.5] |
|  | 53 | 50A2/30S/20C | 3.9 | 25.0 | 42.0 | 57.3 | 69.6 | 91.4 | (23.5) [34.0] | (34.4) [43.2] | (44.1) [57.7] | (45.3) [63.9] |
|  | 54 | 50C2/30S/20C | 3.8 | 22.1 | 42.2 | 62.3 | 70.5 | 76.3 | (29.0) [29.0] | (38.5) [42.8] | (50.0) [55.6] | (60.0) [63.3] |
|  | 55 | 50C5/30S/20C | 3.0 | 19.1 | 34.4 | 60.3 | 72.1 | 94.8 | (24.5) [26.0] | (34.1) [36.7] | (46.7) [50.9] | (54.4) [59.1] |
|  | 56 | 50D2/30S/20C | 0.5 | 20.3 | 34.5 | 42.1 | 64.2 | 75.5 | (22.7) [21.6] | (31.4) [35.3] | (42.0) [40.9] | (44.7) [46.4] |
|  | 57 | 50D3/30S/20C | 2.4 | 23.2 | 36.8 | 57.9 | 61.4 | 86.9 | (23.6) [26.3] | (32.5) [35.8] | (40.9) [41.9] | (50.2) [46.3] |
|  | 58 | 50E2/30S/20C | 4.0 | 26.2 | 42.3 | 64.0 | 69.2 | 73.0 | (20.0) [27.9] | (29.0) [42.5] | (36.3) [52.0] | (41.2) [59.3] |
| I | 59 | 50A1/30S/20F | 4.9 | 20.4 | 30.7 | 42.7 | 53.0 | 66.1 | (21.2) [34.3] | (30.9) [47.9] | (37.5) [57.6] | (42.6) [64.5] |
|  | 60 | 50C1/30S/20F | 3.2 | 11.7 | 21.3 | 39.4 | 53.5 | 73.0 | (21.8) [25.2] | (32.2) [41.9] | (44.6) [53.2] | (51.6) [61.8] |
|  | 61 | 50D1/30S/20F | 4.4 | 18.8 | 28.3 | 42.2 | 54.1 | 69.4 | (25.1) [28.4] | (34.9) [44.0] | (41.6) [54.9] | (47.4) [62.0] |
|  | 62 | 50E1/30S/20F | 3.7 | 20.8 | 32.6 | 44.6 | 57.0 | 76.7 | (24.0) [28.6] | (35.4) [38.4] | (43.6) [50.6] | (45.8) [56.9] |
|  | 63 | 50A2/30S/20F | 5.0 | 24.6 | 35.1 | 40.7 | 51.2 | 72.1 | (27.6) [36.2] | (39.2) [48.1] | (45.7) [55.3] | (50.6) [61.0] |
|  | 64 | 50C2/30S/20F | 6.5 | --- | --- | --- | --- | --- | (23.0) [34.4] | (32.5) [52.2] | (40.5) [60.5] | (46.9) [66.8] |
|  | 65 | 50C5/30S/20F | 5.1 | 24.8 | 29.1 | 50.8 | 62.7 | 73.5 | (---) [33.5] | (---) [50.0] | (---) [62.1] | (---) [67.2] |
|  | 66 | 50D2/30S/20F | 2.7 | 20.9 | 34.3 | 43.9 | 47.1 | 63.6 | (---) [31.7] | (---) [44.7] | (---) [51.9] | (---) [57.9] |
|  | 67 | 50D3/30S/20F | 4.8 | 23.1 | 29.8 | 48.8 | 58.0 | 70.2 | (26.0) [32.0] | (39.1) [46.4] | (44.6) [53.5] | (50.2) [58.3] |
|  | 68 | 50E2/30S/20F | 5.7 | 25.0 | 37.7 | 49.5 | 56.4 | 64.7 | (21.5) [30.0] | (30.3) [41.4] | (38.3) [47.6] | (37.7) [52.5] |

Notes:	(gravel concrete strengths) [limestone concrete strengths] V5: Mean = 35.5MPa, COV = 26.6%

TABLE 4 Cement Paste and Concrete Compressive Strengths (Mixes 69-106)

| Group | Mix No. | Mix ID | Cement Paste fcp w/cm = 0.50 |  |  |  |  |  | Concrete fc w/cm = 0.43 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1D | 7D | 14D | 28D | 56D | 180D | 7D | 14D | 28D | 56D |
| J | 69 | 40C1/40S/20C | 1.3 | 8.6 | 16.7 | 38.3 | 47.6 | 73.0 | (15.3) [---] | (25.2) [---] | (34.9) [---] | (42.4) [---] |
|  | 70 | 40C2/40S/20C | 2.3 | 13.5 | 25.0 | 43.6 | 55.3 | 68.1 | (19.3) [---] | (29.9) [---] | (41.3) [---] | (44.1) [---] |
| K | 71 | 40C1/30S/30C | 1.1 | 7.9 | 12.4 | 26.2 | 46.3 | 65.1 | (14.9) [---] | (21.1) [---] | (33.7) [---] | (39.5) [---] |
|  | 72 | 40C2/30S/30C | 1.9 | 11.7 | 16.9 | 32.7 | 54.2 | 73.4 | (16.2) [---] | (21.8) [---] | (34.6) [---] | (44.3) [---] |
| L | 73 | 40C1/50S/10C | 1.4 | 8.6 | 24.6 | 60.6 | 66.0 | 88.6 | (10.2) [---] | (25.4) [---] | (33.5) [---] | (43.9) [---] |
|  | 74 | 40C2/50S/10C | 2.2 | 18.7 | 41.9 | 52.3 | 63.8 | 77.5 | (20.7) [---] | (34.9) [---] | (43.4) [---] | (44.8) [---] |
| M | 75 | 40C1/0S/60C | 0.3 | 7.1 | 9.2 | 11.9 | 25.1 | 39.1 | (11.6) [---] | (14.9) [---] | (19.5) [---] | (25.7) [---] |
|  | 76 | 40C2/0S/60C | 0.7 | 12.0 | 16.0 | 19.4 | 29.6 | 47.2 | (13.3) [---] | (16.9) [---] | (19.7) [---] | (25.2) [---] |
| N | 77 | 40C1/60S/0C | 1.7 | 10.8 | 37.5 | 52.7 | 68.0 | 70.0 | (22.2) [---] | (41.6) [---] | (50.2) [---] | (57.1) [---] |
|  | 78 | 40C2/60S/0C | 1.2 | 30.8 | 46.2 | 66.4 | 76.6 | 83.0 | (35.4) [---] | (43.9) [---] | (50.5) [---] | (50.7) [---] |
| O | 79 | 30C1/60S/10C | 0.8 | 7.2 | 26.0 | 60.9 | 80.1 | 98.0 | (13.2) [---] | (17.4) [---] | (39.8) [---] | (57.7) [---] |
|  | 80 | 30C2/60S/10C | 1.3 | 19.7 | 50.4 | 53.0 | 67.0 | 77.8 | (17.6) [---] | (26.2) [---] | (28.8) [---] | (32.4) [---] |
|  | 81 | 30C3/60S/10C | 1.0 | 21.0 | 50.0 | 79.6 | 77.7 | 77.7 | (18.1) [---] | (34.8) [---] | (40.9) [---] | (44.4) [---] |
|  | 82 | 30C4/60S/10C | 1.3 | 6.7 | 20.6 | 57.3 | 81.4 | 78.3 | (9.0) [---] | (20.8) [---] | (44.2) [---] | (58.0) [---] |
|  | 83 | 30C5/60S/10C | 3.6 | 16.2 | 41.7 | 59.6 | 82.8 | --- | (23.1) [---] | (34.2) [---] | (43.0) [---] | (48.2) [---] |
| P | 84 | 30C1/70S/0C | 1.0 | 8.4 | 36.4 | 42.9 | 63.4 | 62.6 | (14.9) [---] | (32.6) [---] | (35.1) [---] | (42.2) [---] |
|  | 85 | 30C2/70S/0C | 1.6 | 29.0 | 51.5 | 63.9 | 73.4 | 60.9 | (24.4) [---] | (30.6) [---] | (34.8) [---] | (35.6) [---] |
| Q | 86 | 30C3/50S/20C | 0.9 | 7.8 | 27.8 | 57.1 | 76.7 | 71.2 | (10.4) [---] | (22.8) [---] | (31.4) [---] | (38.5) [---] |
|  | 87 | 30C4/50S/20C | 1.0 | 4.9 | 8.4 | 35.2 | 73.7 | 96.5 | (8.8) [---] | (12.3) [---] | (33.3) [---] | (49.9) [---] |
|  | 88 | 30A1/50S/20C | 0.7 | 6.6 | 12.2 | 44.9 | 65.5 | 89.4 | (7.2) [14.3] | (11.1) [33.4] | (30.8) [52.6] | (44.0) [54.8] |
|  | 89 | 30C1/50S/20C | 0.6 | 6.3 | 10.9 | 43.3V6 | 71.1 | 94.1 | (11.1) [14.6] | (16.5) [28.5] | (41.2) [38.8] | (54.6) [51.6] |
|  | 90 | 30D1/50S/20C | 0.7 | 10.1 | 20.1 | 47.9 | 56.9 | 80.6 | (7.8) [11.7] | (13.8) [24.4] | (30.8) [46.2] | (40.4) [59.3] |
|  | 91 | 30E1/50S/20C | 0.8 | 8.1 | 13.0 | 38.6 | 49.1 | 53.5 | (7.1) [13.8] | (17.0) [34.4] | (32.3) [50.5] | (40.6) [57.2] |
|  | 92 | 30A2/50S/20C | 0.8 | 14.2 | 34.5 | 56.6 | 76.3 | 94.2 | (11.0) [18.9] | (24.3) [38.3] | (37.9) [47.6] | (45.3) [59.5] |
|  | 93 | 30C2/50S/20C | 0.8 | 10.1 | 29.9 | 54.5 | 79.1 | 67.1 | (12.3) [14.5] | (23.9) [39.4] | (37.6) [47.6] | (40.7) [55.0] |
|  | 94 | 30C5/50S/20C | 0.9 | 12.3 | 33.6 | 51.8 | 72.6 | 91.3 | (10.7) [13.9] | (27.2) [42.2] | (42.9) [48.5] | (50.1) [61.5] |
|  | 95 | 30D2/50S/20C | 0.2 | 13.1 | 28.2 | 44.0 | 60.1 | 72.7 | (9.9) [13.8] | (17.8) [34.0] | (36.0) [51.4] | (42.8) [59.4] |
|  | 96 | 30D3/50S/20C | 0.6 | 14.7 | 34.7 | 53.8 | 71.6 | 84.4 | (11.0) [15.4] | (24.5) [32.1] | (35.8) [43.3] | (42.8) [49.2] |
|  | 97 | 30E2/50S/20C | 1.4 | 14.9 | 38.0 | 55.3 | 66.5 | 85.8 | (12.7) [14.9] | (24.3) [29.8] | (30.3) [37.4] | (35.2) [46.6] |
| R | 98 | 30A1/50S/20F | 2.5 | 14.4 | 32.8 | 45.8 | 59.2 | --- | (---) [30.1] | (---) [44.7] | (---) [51.8] | (---) [57.8] |
|  | 99 | 30C1/50S/20F | 2.7 | 10.0 | 25.0 | 38.8 | 56.9 | --- | (---) [23.5] | (---) [45.0] | (---) [56.1] | (---) [62.5] |
|  | 100 | 30D1/50S/20F | 2.8 | 13.9 | 31.5 | 52.5 | 66.8 | --- | (---) [30.0] | (---) [43.9] | (---) [50.6] | (---) [56.9] |
|  | 101 | 30E1/50S/20F | 2.6 | 16.3 | 24.6 | 54.7 | 65.7 | --- | (---) [27.6] | (---) [38.1] | (---) [43.6] | (---) [48.4] |
|  | 102 | 30A2/50S/20F | 3.1 | 22.7 | 39.1 | 47.0 | 60.3 | --- | (---) [30.8] | (---) [44.0] | (---) [48.6] | (---) [53.8] |
|  | 103 | 30C5/50S/20F | 2.9 | 20.8 | 37.6 | 54.5 | 66.0 | --- | (---) [30.9] | (---) [44.4] | (---) [49.8] | (---) [54.2] |
|  | 104 | 30D2/50S/20F | 2.6 | 19.9 | 38.0 | 45.7 | 64.3 | --- | (---) [30.0] | (---) [41.9] | (---) [47.3] | (---) [52.2] |
|  | 105 | 30D3/50S/20F | 2.6 | 17.4 | 39.0 | 55.0 | 63.8 | --- | (---) [33.2] | (---) [42.8] | (---) [48.9] | (---) [54.1] |
|  | 106 | 30E2/50S/20F | 3.1 | 22.7 | 42.6 | 56.0 | 62.7 | --- | (---) [29.2] | (---) [38.4] | (---) [42.7] | (---) [45.7] |

Notes:	(gravel concrete strengths) [limestone concrete strengths] V6: Mean = 33.3MPa, COV = 19.2%

TABLE 5 Cement Paste Compressive Strengths with Varying Water to Cementitious Ratios

| Group | Mix No. | Mix ID | 0.40 w/cm fcp (MPa) |  |  |  |  |  | 0.43 fcp w/cm (MPa) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1D | 7D | 14D | 28D | 56D | 180D | 1D | 7D | 14D | 28D | 56D | 180D |
| A | 1 | 100C1/0S/0C | 32.7 | 56.6 | 58.9 | 72.9 | 76.7 | 81.5 | 26.2 | 47.3 | 47.2 | 59.8 | 71.6 | 74.3 |
|  | 3 | 100C4/0S/0C | 37.2 | 58.8 | 68.0 | 75.1 | --- | 89.4 | 32.6 | 51.9 | 61.6 | 66.4 | --- | 82.1 |
|  | 4 | 100A1/0S/0C | 32.7 | 52.5 | 63.6 | 67.2 | 76.5 | 77.4 | 23.2 | 44.9 | 52.0 | 61.1 | 69.3 | 70.8 |
|  | 5 | 100D1/0S/0C | 28.4 | 47.6 | 61.9 | 66.8 | 72.6 | 73.7 | 25.3 | 44.5 | 50.4 | 58.9 | 65.3 | 72.6 |
|  | 6 | 100E1/0S/0C | 29.4 | 52.9 | 60.1 | 67.6 | 66.7 | 74.2 | 23.2 | 44.6 | 49.2 | 62.5 | 55.2 | 65.7 |
|  | 7 | 100A2/0S/0C | 32.7 | 54.3 | 61.4 | 66.8 | 73.8 | 76.8 | 29.4 | 52.4 | 55.4 | 62.2 | 65.2 | 72.5 |
|  | 9 | 100C5/0S/0C | 35.9 | 54.3 | 66.7 | 78.4 | 77.1 | 79.6 | 29.5 | 53.7 | 61.7 | 65.0 | 71.4 | 66.8 |
|  | 10 | 100D2/0S/0C | 24.3 | 55.3 | 63.9 | 66.6 | 71.5 | 73.1 | 19.4 | 43.0 | 54.8 | 54.8 | 50.4 | 61.9 |
|  | 11 | 100D3/0S/0C | 34.3 | 56.2 | 68.4 | 72.0 | 77.0 | 79.9 | 29.7 | 52.3 | 57.5 | 51.9 | 65.3 | 72.1 |
|  | 12 | 100E2/0S/0C | 35.1 | 63.3 | 75.0 | 78.4 | 79.2 | 81.2 | 32.0 | 46.5 | 62.4 | 66.3 | 64.8 | 70.0 |
| F | 37 | 50C1/40S/10C | --- | 21.5 | 54.3 | 73.9 | 90.2 | 98.7 | --- | (20.5) | (48.0) | (67.5) | (81.6) | --- |
|  | 38 | 50C2/40S/10C | --- | 49.6 | 74.5 | 89.5 | 112.2 | 93.2 | --- | (42.5) | (67.2) | (80.8) | (100.1) | --- |
|  | 39 | 50C3/40S/10C | --- | 40.6 | 63.1 | 81.9 | 90.6 | 107.2 | --- | (35.6) | (58.0) | (77.4) | (88.7) | --- |
|  | 40 | 50C4/40S/10C | --- | 28.6 | 51.3 | 69.3 | 85.1 | 110.0 | --- | (23.5) | (43.0) | (65.8) | (85.0) | --- |
| G | 42 | 50C1/25S/25C | --- | 22.6 | 37.3 | 61.4 | 86.7 | 99.9 | --- | (19.5) | (31.7) | (55.3) | (79.2) | --- |
|  | 43 | 50C2/25S/25C | --- | 39.6 | 60.7 | 73.9 | 100.5 | 109.5 | --- | (34.2) | (52.1) | (67.6) | (91.1) | --- |
|  | 44 | 50C3/25S/25C | --- | 31.6 | 51.4 | 62.4 | 96.0 | 70.6 | --- | (27.6) | (44.8) | (57.2) | (86.9) | --- |
|  | 45 | 50C4/25S/25C | --- | 36.1 | 51.4 | 64.5 | 82.0 | 102.6 | --- | (28.9) | (41.7) | (58.8) | (75.5) | --- |
|  | 47 | 50C3/30S/20C | --- | 33.4 | 52.7 | 70.2 | 91.0 | 85.9 | --- | (29.6) | (47.7) | (67.3) | (86.8) | --- |
|  | 48 | 50C4/30S/20C | --- | 25.4 | 46.2 | 64.7 | 83.9 | 98.7 | --- | (22.0) | (38.4) | (57.8) | (74.5) | --- |
| H | 49 | 50A1/30S/20C | --- | 37.2 | 47.7 | 62.1 | 73.9 | --- | --- | 31.5 | 38.4 | 59.7 | 62.0 | --- |
|  | 50 | 50C1/30S/20C | --- | 22.2 | 42.0 | 67.8 | 84.7 | 72.3 | --- | 24.9 | 32.1 | 48.2 | 56.6 | --- |
|  | 51 | 50D1/30S/20C | --- | 35.7 | 45.9 | 66.3 | 68.1 | --- | --- | 29.7 | 35.7 | 56.3 | 53.8 | --- |
|  | 52 | 50E1/30S/20C | --- | 35.7 | 54.2 | 58.4 | 79.6 | --- | --- | 30.3 | 43.0 | 37.3 | 53.4 | --- |
|  | 53 | 50A2/30S/20C | --- | 46.3 | 63.0 | 80.7 | 81.5 | --- | --- | 40.8 | 53.6 | 71.4 | 73.4 | --- |
|  | 54 | 50C2/30S/20C | --- | 43.9 | 65.9 | 80.9 | 73.7 | 78.1 | --- | (37.4) | (58.8) | (75.3) | (72.7) | --- |
|  | 55 | 50C5/30S/20C | --- | 43.5 | 56.6 | 79.1 | 72.7 | --- | --- | 38.9 | 47.7 | 68.0 | 84.7 | --- |
|  | 56 | 50D2/30S/20C | --- | 41.3 | 54.9 | 69.9 | 71.1 | --- | --- | 34.3 | 45.8 | 49.4 | 76.1 | --- |
|  | 57 | 50D3/30S/20C | --- | 46.2 | 68.6 | 87.6 | 80.2 | --- | --- | 39.1 | 55.6 | 71.5 | 79.5 | --- |
|  | 58 | 50E2/30S/20C | --- | --- | --- | --- | --- | --- | --- | 41.6 | 58.4 | 74.5 | 87.0 | --- |
| O | 79 | 30C1/60S/10C | --- | 11.4 | 41.1 | 71.5 | 84.3 | 99.9 | --- | (10.1) | (36.6) | (68.3) | (83.0) | --- |
|  | 80 | 30C2/60S/10C | --- | 33.1 | 67.5 | 90.4 | 106.1 | 121.1 | --- | (29.1) | (62.4) | (79.2) | (94.4) | --- |
|  | 81 | 30C3/60S/10C | --- | 33.8 | 61.5 | 79.6 | 84.8 | 100.0 | --- | (29.9) | (58.1) | (79.6) | (82.7) | --- |
|  | 82 | 30C4/60S/10C | --- | 10.7 | 33.2 | 53.4 | 85.0 | 105.6 | --- | (9.5) | (29.4) | (54.6) | (83.9) | --- |
| Q | 86 | 30C3/50S/20C | --- | 14.6 | 37.2 | 71.2 | 76.0 | 100.7 | --- | (12.5) | (34.4) | (67.0) | (76.2) | --- |
|  | 87 | 30C4/50S/20C | --- | 8.7 | 15.7 | 55.6 | 85.0 | 109.7 | --- | (7.6) | (13.5) | (49.5) | (81.7) | --- |
|  | 88 | 30A1/50S/20C | --- | 22.7 | 32.9 | 48.4 | 82.4 | --- | --- | 20.4 | 22.9 | 43.1 | 73.9 | --- |
|  | 89 | 30C1/50S/20C | --- | 9.7 | 20.6 | 65.2 | 77.1 | 72.3 | --- | 14.9 | 17.6 | 43.2 | 59.9 | --- |
|  | 90 | 30D1/50S/20C | --- | 23.7 | 33.1 | 58.2 | 82.6 | --- | --- | 18.5 | 25.5 | 51.6 | 82.4 | --- |
|  | 91 | 30E1/50S/20C | --- | 18.9 | 32.8 | 46.5 | 93.9 | --- | --- | 16.9 | 25.0 | 50.2 | 76.0 | --- |
|  | 92 | 30A2/50S/20C | --- | 31.6 | 46.9 | 71.0 | 93.6 | --- | --- | 25.4 | 38.0 | 66.2 | 72.8 | --- |
|  | 93 | 30C2/50S/20C | --- | 19.8 | 50.6 | 72.8 | 106.3 | 114.6 | --- | (16.9) | (44.4) | (67.3) | (98.1) | --- |
|  | 94 | 30C5/50S/20C | --- | 32.2 | 49.0 | 71.6 | 82.2 | --- | --- | 29.5 | 40.5 | 66.1 | 59.8 | --- |
|  | 95 | 30D2/50S/20C | --- | --- | --- | --- | --- | --- | --- | 20.4 | 27.0 | 45.6 | 40.1 | --- |
|  | 96 | 30D3/50S/20C | --- | 32.0 | 54.9 | 67.5 | 55.6 | --- | --- | 26.9 | 45.0 | 69.1 | 65.7 | --- |
|  | 97 | 30E2/50S/20C | --- | --- | --- | --- | --- | --- | --- | 28.1 | 42.3 | 76.4 | 59.2 | --- |

Notes:	(linearly predicted strength) explained elsewhere in the paper

TABLE 6 t-test Results Relative to Fig. 4

| Case |  | n | VAR1 | VAR2 | AMD (MPa) | p-value | Test Variable |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | GR | 16 | A-OPC | A-PLC | -0.4 | 0.58 | GR – OPC vs. PLC No SCM |
| 2 | GR | 16 | B-OPC | B-PLC | -11.9 | < 0.01 | GR – OPC vs. PLC 40%C |
| 3 | GR | 16 | H-OPC | H-PLC | -4.5 | < 0.01 | GR – OPC vs. PLC 50/30S/20C |
| 4 | GR | 16 | I-OPC | I-PLC | -0.8 | 0.54 | GR – OPC vs. PLC 50/30S/20F |
| 5 | GR | 16 | Q-OPC | Q-PLC | -2.7 | 0.12 | GR – OPC vs. PLC 30/50S/20C |
| 6 | LS | 16 | A-OPC | A-PLC | 0.5 | 0.52 | LS – OPC vs. PLC No SCM |
| 7 | LS | 16 | B-OPC | B-PLC | -7.6 | < 0.01 | LS – OPC vs. PLC 40%C |
| 8 | LS | 15 | C-OPC | C-PLC | 0.1 | 0.94 | LS – OPC vs. PLC 40%F |
| 9 | LS | 16 | H-OPC | H-PLC | -5.2 | < 0.01 | LS – OPC vs. PLC 50/30S/20C |
| 10 | LS | 16 | I-OPC | I-PLC | -1.6 | 0.18 | LS – OPC vs. PLC 50/30S/20F |
| 11 | LS | 16 | Q-OPC | Q-PLC | -0.6 | 0.77 | LS – OPC vs. PLC 30/50S/20C |
| 12 | LS | 12 | R-OPC | R-PLC | -0.4 | 0.16 | LS – OPC vs. PLC 30/50S/20F |
| 13 | CP | 16 | A-OPC | A-PLC | -2.2 | 0.25 | CP – OPC vs. PLC No SCM |
| 14 | CP | 16 | B-OPC | B-PLC | -10.2 | < 0.01 | CP – OPC vs. PLC 40%C |
| 15 | CP | 12 | C-OPC | C-PLC | -1.8 | 0.01 | CP – OPC vs. PLC 40%F |
| 16 | CP | 16 | H-OPC | H-PLC | -9.1 | < 0.01 | CP – OPC vs. PLC 50/30S/20C |
| 17 | CP | 12 | I-OPC | I-PLC | -2.9 | < 0.01 | CP – OPC vs. PLC 50/30S/20F |
| 18 | CP | 16 | Q-OPC | Q-PLC | -12.5 | < 0.01 | CP – OPC vs. PLC 30/50S/20C |
| 19 | CP | 12 | R-OPC | R-PLC | -4.2 | 0.03 | CP – OPC vs. PLC 30/50S/20F |
| 20 | GR | 16 | A-OPC | B-OPC | 15.3 | < 0.01 | GR – fc-GR loss with OPC and 40%C |
| 21 | GR | 16 | A-PLC | B-PLC | 3.8 | 0.04 | GR – fc-GR loss with PLC and 40%C |
| 22 | LS | 12 | B-PLC | C-PLC | 13.4 | < 0.01 | LS – Effect of 40%C and F ash with LS |
| 23 | LS | 16 | H-OPC | I-OPC | -6.9 | < 0.01 | LS – Effect of 20%C and F ash with 30%S |
| 24 | CP | 16 | B-OPC | C-OPC | 6.2 | < 0.01 | CP – Effect of 40%C and F ash with CP |
| 25 | CP | 12 | B-PLC | C-PLC | 13.6 | < 0.01 | CP – Effect of 20%C and F ash with 30%S |

Note: 	Average Mean Difference (AMD) was always Var1-Var2

Var1 = variable 1 e.g. A-OPC is all OPC in group A, Var2 = variable 2

List of Figures

Fig. 1 - Cement paste laboratory operations pictures

Fig. 2 - Frequency histogram of R2 values for fcp at varying w/cm

Fig. 3 - Global plots considering all Table 2 to 4 data where pairs could be made

Fig. 4 - OPC and PLC comparisons of GR concrete, LS concrete, and CP strengths

Fig. 5 - Concrete versus Cement Paste at 0.43 w/cm ratio

Fig. 6 - Concrete versus cement paste bar charts at 0.43 w/cm ratio

PhD Candidate, Civil and Environmental Engineering, Mississippi State University, 501 Hardy Road, Mail Stop 9546, Mississippi State, MS 39762, ORCID: 0000-0002-9336-3825 (Corresponding Author) Email: bh710@cavs.msstate.edu

Research Civil Engineer, U.S. Army Corps Engineer Research and Development Center, 3909 Halls Ferry Rd., Vicksburg, MS 39180, ORCID: 0000-0001-5601-8830

Materials and Construction Industries Chair, Civil and Environmental Engineering, Mississippi State University, 501 Hardy Road-Mail Stop 9546, Mississippi State, MS 39762, ORCID: 0000-0003-4642-7723